## Slide 1
Ion Exchange Control Drug Delivery System

## Slide 2
Controlled drug delivery systems are gaining momentum in the recent two decades. One of the attractive methods for modified drug delivery systems is the use of ion exchange resins(IER) a carriers for such systems .
Ion Exchange Resins (IER) are insoluble polymers that contain acidic or basic functional groups and have the ability to exchange counter-ions within aqueous solutions surrounding them.
An ion exchange resin is exhibited like small bead with a diameter between 1-2 mm
Ion exchange is a reversible process in which ions of like sign are exchanged between liquid and solid when in contact with a highly insoluble body
INTRODUCTION
An ion-exchange resin or ion-exchange polymer is a resin or polymer that acts as a medium for ion exchange. It is an insoluble matrix (or support structure) normally in the form of small (0.25–0.5 mm radius) microbeads, usually white or yellowish, fabricated from an organic polymer substrate. The beads are typically porous, providing a large surface area on and inside them. The trapping of ions occurs along with the accompanying release of other ions, and thus the process is called ion exchange. There are multiple types of ion-exchange resin. Most commercial resins are made of polystyrene sulfonate
https://www.samcotech.com/ion-exchange-resin-work-process/

## Slide 3
The drug is released from the resinate by exchanging with ions in the gastrointestinal fluid, followed by drug diffusion
Due to the presence of high molecular weight water insoluble polymers, resins are not absorbed by the body and are therefore inert
Drug resinates are generally prepared with purified resins and appropriate drugs.
Ion-exchange systems are advantageous for drugs that are highly susceptible to degradation by enzymatic process.
Furthermore, if well maintained, resin beds can last for many years before replacement
However, the limitation is that the release rate is proportional to the concentration of the ions present in the area of administration. More so, the release rate of drug can be affected by variability in diet, water intake and individual intestinal content.

## Slide 4
STRUCTURE AND CHEMISTRY OF ION EXCHANGE RESIN
IER are simply insoluble polyelectrolytes that are insoluble polymers which contain ionizable groups distributed regularly along the polymer backbone.
The most common resins used in formulations are;
  Cross-linked polystyrene
  Polymethacrylate polymers
When IER are mixed with a fluid such as water, ions in the fluid can exchange with the polyelectrolyte’s counterions and be physically removed from the fluid
An ion exchange resin is a polymer (normally styrene) with electrically charged sites at which one ion may replace another. There are numerous functional groups that have charge, only a few are commonly used for man-made IER.
These are:
  -COOH, which is weakly ionized to -COO¯,
  -SO3H, which is strongly ionized to -SO3¯,
  -NH2, which weakly attracts protons to form NH3+ -secondary and tertiary amines that also attract protons weakly,
  NR3+ which has a strong, permanent charge (R stands for some organic group).
These groups are sufficient to allow selection of a resin with either weak or strong positive or negative charge.

## Slide 5
TYPES OF ION-EXCHANGE RESINS
There are two major classes of ion-exchange polymers. These are discussed in the following two sub-sections.
Catoin IER:
  Strong acid
  Weak acid
Anioin IER:
  Strong basic
  Weak basic

## Slide 6
CATION EXCHANGE RESINS
Cation exchange resins contain covalently bound negatively charged functional groups and exchanges positively charged ions.
There are prepared by the copolymerization of styrene and divinyl benzene and have sulfonic acid groups (-SO3H) introduced into most of the benzene rings .
The mechanism of cation exchange process can be represented by the following reaction in Eq R- - ex+ + C+ →R- - C+ + ex+
where, R is a resin polymer with SO3-sites available for bonding with exchangeable cation (ex+), and C+ indicates a cation in the surrounding solution getting exchanged

## Slide 7
STRONG ACID CATION EXCHANGE RESINS
The chemical behaviour of these resins is similar to that of a strong acid. These resins are highly ionized in both the acid (R-SO3H) and salt (RSO3Na) form of the sulfonic acid group (-SO3H).
They can convert a metal salt to the corresponding acid by the reaction in Eq. 2(R-SO3H) + NaCl2 → (R-SO4) Na + 2HCl The hydrogen and sodium forms of strong acid resins are highly dissociated, and the exchangeable Na+and H+ are readily available for exchange over the entire pH range.
Consequently, the exchange capacity of strong acid resins is independent of the solution

## Slide 8
WEAK ACID CATION EXCHANGE RESINS
These resins behave similarly to weak organic acids that are weakly dissociated.
In a weak acid resin the ionisable group is a carboxylic acid (COOH) as opposed to the sulfonic acid group (SO3H) used in strong acid resins. The degree of dissociation of a weak acid resin is strongly influenced by the solution pH.
Consequently, resin capacity depends in part on the solution pH. A typical weak acid resin has limited capacity below a pH of 6.0.

## Slide 9
ANION EXCHANGE RESINS
Anion exchange resins have positively charged functional groups and there exchanges negatively charged ions. These are prepared by first chlormethylating the benzene rings of styrene-divinylbenzene copolymer to attach CH2Cl groups and then causing these to react with tertiary amines such as triethylamine. The mechanism of anion exchange process can be Represented by the following reaction in Eq. R+ - ex - + A- → R+- A- + ex- where, R+ indicates a resin polymer with number of sites available for bonding with exchangeable anion (ex-), and A- indicates cations in the surrounding solution getting exchanged.

## Slide 10
STRONG BASE ANION EXCHANGE RESINS
Strong base resins are highly ionized and can be used over the entire pH range
These resins are used in the hydroxide (OH) form for water deionization
They will react with anions in solution and can convert an acid solution to pure water Eq. R-NH3OH + HCl → R-NH3Cl + H2O
Regeneration with concentrated sodium hydroxide (NaOH) converts the exhausted resin to the OH form.

## Slide 11
WEAK BASE ANION EXCHANGE RESIN
Weak base resins are like weak acid resins in that the degree of ionization is strongly influenced by pH.
Hence, weak base resins exhibit minimum exchange capacity pH of 7.0.
The weak base resin does not have an OH ion form as does the strong base resin Eq.
R-NH2 + HCl → R-NH3Cl
Consequently, regeneration needs only to neutralize the absorbed acid; it need not provide OH ions.
Less expensive weakly basic reagents such as ammonia (NH3) or sodium carbonate can be employed

## Slide 12
ROLE OF IER IN CONTROLLED DRUG DELIVERY SYSTEMS
The major drawback of controlled release is dose dumping, resulting in increased risk of toxicity.
The usage of IER during the development of controlled release formulations plays a significant role because of their drug retarding properties and prevention of dose dumping.
The drug resinates can also be used as a drug reservoir, which has caused a change of the drug release in hydrophilic polymer
The use of IER into drug delivery systems have been encouraged because of their
  Physico-chemical stability,
  Inert nature,
  Uniform size,
  Spherical shape assisting coating and
  Equilibrium driven reproducible drug release in ionic environment .
The physical and chemical properties of the IER will release the drug more uniformly than that of simple matrix system.

## Slide 13
Drug molecules attached to the resins are released by appropriate charged ions in the gastrointestinal tract, followed by diffusion of free drug molecules out of the resin as: Resin- Drug+ + X+----- Resin-X+ + Drug+
Resin+ Drug-+ Y- ---- Resin+Y- + Drug-
  where, X and Y are ions in the gastrointestinal tract
IER have been used as drug carriers in pharmaceutical dosage forms for controlled release formulation
The prolonged release of the active drug is accomplished by;
  Providing a semi-permeable coating around discrete, minute, ion exchange resin particles with which the drug component has been complexed to form an insoluble drug resin complex. The semi-permeable coating creates a diffusion barrier and the thickness of which can be adjusted to provide the desired level of retardation of drug availability in the gastrointestinal tract over a period of time .
  Several preparations involving strong resonates of sulphuric acid (cation exchange resins) provided more moderate release than the weak resinates of carboxylic acid. Hence, resinates of strong cationic drugs are formulated as sustained release suspension, tablets, capsules and micro particles.

## Slide 14: MECHANISM AND PRINCIPLE
Anion exchange resins involve basic functional groups capable of removing anions from acidic solutions while Cation exchange resins contain acidic functional group, capable of removing cations from basic solutions.
The use of IER to prolong the effect of drug release is based on the principle that positively or negatively charged pharmaceuticals, combined with appropriate resins to yield insoluble polysalt resinates. R-SO-3 H+ + H2N-A ↔ R-SO-3 – H3N-A
R-N+H3OH- + HOOC-B ↔ R-N+H3 –OOC-B + H2O
  H2N-A → basic drug
  R-SO-3H+ → cation exchanges
  HOOC-B → acidic drug R-NH3+OH- → anion exchange resins
Ion exchange resinates administered orally are likely to spend about two hours in the stomach in contact with an acidic fluid of pH 1.2, and then move into the intestine where they will be in contact for several hours with a fluid of slightly alkaline pH

## Slide 15
IN THE STOMACH
R-SO-3 - H3 N+-A + HCl ↔ R-SO3-H+ + A-N+H3Cl
R-N+H3-OOC-B + HCl ↔ R-N+H3Cl+ + B-COOH
IN THE INTESTINE
R-SO-3 - H3 N-A +NaCl ↔ R-SO3-Na+ +A-N+H3Cl-
R-N+H3- OOC-B +NaCl ↔ R-N+H3Cl- + B-COO-Na+

## Slide 16: IMPORTANT PROPERTIES OF IER
During the process of developing formulations with IER, some of the important properties normally considered by researchers include the following:
Particle size and form:
The rate of ion-exchange reactions depends on the size of the resin particles. Decreasing the size of resin particle significantly decreases the time required for the reaction to reach equilibrium with the surrounding medium
Porosity and swelling:
Porosity is defined as the ratio of the volume of the material to its mass. The size of the ions, which can penetrate into a resin matrix, depends strongly on the porosity. Porosity of the ion-exchangers depends upon polymerization procedures. The amount of swelling is directly proportional to the number of hydrophilic functional groups attached to the polymer matrix and is inversely proportional so the degree of divinyl benzene cross linking present in the resin .
Cross linkage:
The percentage of cross linking affects the purely physical structure of the resin particles. The degree of cross linkage is controlled by the percent of divinylbenzene (DVB) used in the copolymerization. The fraction of DVB determines to what extent the ion exchange resin is free to swell and shrink. The swelling in turn affects the rate of hydration .

## Slide 17
Available capacity:
The capacity of an ion-exchanger is a quantitative measure of its ability to take up exchangeable counter-ions and is therefore a major importance. The exchange capacity refers to the number of ionic sites per unit weight or volume. The weight basis value is highly hydrated. The exchange capacity may limit the amount of drug that may be absorbed on a resin and hence the potency of a complex. Carboxylic acid resins derived from acrylic acid polymers have higher exchange capacities than sulphonic acid or amine resins because of bulkier ionic substituent’s and the polystyrene matrix. Therefore, higher drug percentages may often be achieved with carboxylic acid resins.
Acid base strength:
The acid or base strength of an exchanger is dependent on the various ionogenic groups, incorporated into the resin. The Pka value of the resin will have a significant influence on the rate at which the drug will be released from resinate in the gastric fluids

## Slide 18
Stability:
The resinous ion-exchangers are remarkably inert substances. At ordinary temperature and excluding the more potent oxidizing agents, vinylbenzene cross-linked resins are resistant to decomposition through chemical attack. Purity and toxicity:
Since drug resin combinations contain 60% or more of the resin, it is necessary to establish toxicity of the ion-exchange resins. Commercial product cannot be used as such because they contain impurities that cause severe toxicity .Therefore, careful purification of the resin prior to treatment with the drug is required.

## Slide 19
Applications
  Taste Masking
  Excessive bitterness of the active principal ingredients (APIs)n oral formulations is the major taste problem faced by the pharmaceutical industry. Bitterness of formulations can influence selection by physicians and markedly affect patient compliance. Masking of the unpleasant taste of a drug improves compliance and product value. Amongst the numerous available taste-masking methods, ion exchange resins are inexpensive and can be used to develop a simple, rapid and cost-effective method of taste masking

## Slide 20
  Tablet Disintegrant
  Ion exchange resins, because of their excellent swelling property when immersed in water, can be used as a tablet disintegrating agent.
  Drug Stabilization
  The drug resinate is frequently more stable than the original drug. Vitamin B12 has a shelf-life of only a few months, but the resinate is stable for more than two years.
  Another example is nicotine; it discolors quickly on exposure to air and light, but the resinate, used in nicotine chewing gums and lozenges, is much more stable.

## Slide 21
Powder Processing Aid
Hygroscopic drugs are susceptible to agglomeration due to the presence of moisture. Adsorption of such drugs onto ion exchange resins may lead to a decrease in their hygroscopicity. Furthermore, because the resins have a uniform, macroreticular morphology, they provide excellent flowability to the formulation
Deliquescence
Deliquescence can be defined as the conversion of a solid substance into a liquid as a result of absorption of water vapor from the air. Although this is not a common problem, it has been very difficult to solve and requires the use of specialized equipment or careful scheduling of production during dry seasons. However, ion exchange resins may prove instrumental in solving the problem of deliquescence of a drug by the formation of resinate complexes. Sodium valproate, a highly deliquescent drug, has been found to show free flowing properties after complexation with ion exchange resins. The amount of water absorbed decreased with increasing amount of valproate in the resinate. Similar results have been obtained with resinates of rivastigmine bitartrate

## Slide 22
Rapid Dissolution
Ion exchange drug resinate complexes have a faster rate of dissolution. Ion exchange resin matrices are hydrophilic and hence allow water/aqueous solutions to enter the dimensional resin structure, thereby enhancing the dissolution rate. Moreover, each individual drug molecule is bound to a functional site of the resin molecule resulting in reduction of crystal lattice energy, which may be responsible for enhancing the rate of drug dissolution bound to resin

## Slide 23
Factors affecting formulation and drug release from complex
  Cross linking of resin
  Particle size
  pH
  Form of resin
  Size of exchanging ion
  Selectivity of counter-ion
  Mixing time
  Effect of temperature