## Slide 1
Types of Physical vapor deposition techniques
Important physical vapor deposition techniques includes:
Pulsed laser deposition (PLD)
Electron beam evaporation (EBE)
Molecular beam Epitaxy (MBE)
Sputtering

## Slide 2
Pulsed Laser deposition
PLD is very simple technique and produces films with the same composition as the target.
The advantages of pulsed laser deposition are its flexibility, fast response, congruent evaporation and energetic evaporants. While
The basic setup is simple relative to many other deposition techniques
The main drawback of PLD is the formation of droplets in thin film growth, specially when using high laser power.
The physical phenomena of laser-target interaction and film growth are quite complex.

## Slide 3
Working mechanism of PLD
When the laser pulse is absorbed by the target, energy is first converted to thermal energy, resulting in evaporation and plasma formation of target material.The ejected species expand into the surrounding vacuum in the form of a so called plume containing many energetic species including atoms, molecules, electrons, ions, clusters, before depositing on the typically hot substrate.
The process of PLD can schematically be divided into four stages:
Laser evaporation of the target material and creation of a plasma
Dynamic of the plasma under vacuum (expansion, cooling)
Deposition of the ablated material on the substrate
Nucleation and growth of the film on the substrate surface

## Slide 4
Schematic view of pulsed laser deposition (PLD) setup

## Slide 5
Factors effecting deposition rate in PLD
Laser power or Fluence (power or energy per unit surface area)
Laser power or fluence
By increasing the we can increase evaporation and hence deposition rate.
By playing with the focus of lense placed between laser and target material.
Moving towards focus increases the fluence and thus the rate
of evaporation per unit area, however the total area of
evaporation is reduced.

## Slide 6
Thickness of deposited thin film can be measured directly by different microscopy techniques e.g Atomic force microscope (AFM) etc., and indirectly using quartz microbalance etc., explained as below.
A quartz balance in evaporation chamber is used for this purpose. It is a quartz plate whose shear resonance frequency varies depending on rigidity and inertia. The inertia is proportional to quantity of material deposited. Thus, the frequency evolution of the resonance inform us about the quantity of material deposited. Before each deposition, the quartz is placed in front of the target on which laser beam is sent to check the speed of deposition. To deposit required thickness deposition rate is multiplied by time e.g if deposition rate is 1 nm/min, then to deposit 10 nm film we do deposition for 10 minutes, then switched off the laser to stop deposition
Determination of deposited thin film thickness

## Slide 7
There are four types of sputtering process
DC Diode Sputtering
DC Diode Magnetron Sputtering
AC or RF Sputtering
AC or RF Magnetron Sputtering
DC Diode sputtering
Working Mechanism
If a high DC potential difference (~Kilo Volts) is applied between the target (Serving as cathode) and the substrate (serving as anode) in a low pressure Argon environment, electrons released from the target collide with Argon atoms and ionise them, giving them a positive charge. These are then accelerated towards the target and strike it at high energy, releasing target material called “Sputtering”.
Sputtering or Sputter Deposition

## Slide 8
The sputtered material in the form of plasma travel towards substrate and deposite a thin layer of target material on substrate. This Process is called “Sputter Deposition”.
As two electrodes (cathode & Anode) and DC potential are used in this process , so called DC diode sputtering.
However, diode sputtering requires a relatively high process pressure because the electrons follow a short, direct route to the anode (the substrate) so the probability of any given electron striking a given Argon atom (the collisional cross section) is relatively low, and many gas atoms are needed to increase this.
This in turn means that sputtered material goes through many collisions with Ar gas atoms, greatly reducing the amount actually reaching the substrate resulting low deposition rates and much of the target material coats the system rather than the substrate but coverage of uneven or non uniform surfaces can be highly uniform.

## Slide 9
Schematics Sputter deposition Setup

## Slide 10
Schematics Sputter deposition Setup

## Slide 11
Parameters effecting sputter deposition rate
Nature of bombarding Inert gas
Higher the mass or size of bombarding inert gas atoms (Typically Argon is used for sputtering), higher will be the sputter & hence deposition rate resulting rapid thin film coating.
Bombarding Inert gas pressure
Higher the bombarding inert gas pressure, higher will be the sputter & hence deposition rate, resulting rapid thin film coating.
Sputter voltage
Higher the sputter voltage, higher will be the sputter & hence deposition rate, resulting rapid thin film coating
Below threshold voltage no sputtering yield and above and below optimum sputter voltage sputter yield decreases.

## Slide 12
Parameters effecting thin film quality
Substrate Temperature
Usually control with substrate heater, but also changes due to heating from energetic deposited material, which can be decreased with increasing substrate bias or voltage.
Higher or lower substrate tempreature than optimum value can result in rough thin film growth or higher crystallographic defects in film.
Sputtered Plasma Energy
Increases with increasing sputter voltage , decreases with increasing substrate bias, decreases with increasing Ar pressure
Higher or lower sputter plasma atomsor molecules energy than optimum value can result in rough thin film growth or higher crystallographic defects in film.

## Slide 13
Deposition Rate
Increases with Ar pressure, increases with sputter voltage or yield
Higher or lower deposition rates than optimum value can result in rough thin film growth or higher crystallographic defects in film.
Substrate Bias Voltage
Substrate is being bombarded by electrons and ions from target and plasma, so substrate bias can significantly change these parameters & hence thin film properties.

## Slide 14
DC Magnetron sputtering Mechanismsm
If a strong mangetic field is applied along with an electric field, the electrons follow a spiral path around the field lines giving them a much longer path length before being absorbed into a surface.
This greatly increases their chance of striking and ionising an Argon atom and therefore gives the same ion density at a much lower pressure than for diode sputtering.
This allows for much higher deposition rates at much lower Ar pressure and more efficient usage of released material. This technique can be used with both DC or RF voltages.

## Slide 15
AC or radiofrequency (RF) sputtering
When the Argon ion strikes the target an electron is released from the surface and combines with the ion to neutralise it, returning it to the vacuum as an Argon atom. If the target material is dielectric this process rapidly casues a charge buildup at the surface until Argon ions are no longer attracted, electrons are no longer released and the plasma extinguishes.
To sputter nonconducting materials it is therefore necessary to apply AC or pulsed power to the target whereby the ion charge, which has built up on the surface, is expelled during the positive phase. Because the power supply is only negative half the time, rates are lower than for DC sputtering.
To increase sputter rate, complex, imbalance and expensive power supplies are used containing three fourth negative and one fourth positive AC cycle duration instead of balance one half of both positive and negative cycles.

## Slide 16
Schematics AC or radio frequency (RF) sputtering

## Slide 17
Frequency of AC or RF power Supplies
Frequencies less than about 50 kHz
electrons and ions in plasma are mobile
both follow the switching of the anode and cathode
basically DC sputtering of both surfaces
Frequencies above about 50 kHz
ions (heavy) can no longer follow the switching
electrons can neutralize positive charge build up
In AC sputtering, working at frequencies below about 50 kHz, the potential on the target is periodically reversed When potential on target is negative, the ions have enough mobility to reach cathode target before change of potential to do DC diode-like sputtering, while electrons reach the substrate which at that time is at positive potential and results in increase in temprature by depositing their energy there.

## Slide 18
One the other hand after change of polarity on target and substrate i.e when target becomes positive, electrons will move towards target and will neutralize target on which positive charge was accumulated during negative potential at target while ions will travel towards substrate and will do sputtering of film deposited on substrate.
To avoid sputtering of substrate chamber walls are used as counter electrode along with substrate, then most of sputtering will be done at chamber wall instead of substrate and we can protect substrate from sputtering.
At frequencies above 50 kHz, the ions do not have enough mobility to reach the target before change of polarity to allow establishing a dc-diode-like sputtering of target and results in stop of sputtering.

## Slide 19
A major disadvantage of RF sputtering of dielectric targets is that most insulating materials have poor thermal conductivity and high coefficients of thermal expansion, and are usually brittle materials. Since most of the bombarding energy produces heat, this means that large thermal gradients can be generated that result in fracturing the target if high power levels are used.