## Slide 1: Materials & Methods of Construction Properties of Aggregates
Engr. Abdul Rahim Khan

## Slide 2: Properties of Aggregates
Aggregates are used in concrete to provide economy in the cost of concrete. Aggregates act as filler only. These do not react with cement and water.
But there are properties or characteristics of aggregate which influence the properties of resulting concrete mix. These are as follow.

## Slide 3: Composition
Aggregates consisting of materials that can react with alkalies in cement and cause excessive expansion, cracking and deterioration of concrete mix should never be used.
Therefore it is required to test aggregates to know whether there is presence of any such constituents in aggregate or not.

## Slide 4: Size & Shape
The size and shape of the aggregate particles greatly influence the quantity of cement required in concrete mix and hence ultimately economy of concrete.
Maximum size of aggregate should be less than the following Condition

## Slide 5
One-fourth of the minimum dimension of the concrete member.
One-fifth of the minimum dimension of the reinforced concrete member.

## Slide 6: Surface Texture
The development of hard bond strength between aggregate particles and cement paste depends upon the surface texture, surface roughness and surface porosity of the aggregate particles.
If the surface is rough but porous, maximum bond strength develops. In porous surface aggregates, the bond strength increases due to setting of cement paste in the pores.

## Slide 7: Specific Gravity
The ratio of weight of oven dried aggregates maintained for 24 hours at a temperature of 100 to 1100C, to the weight of equal volume of water displaced by saturated dry surface aggregate is known as specific gravity of aggregates.

## Slide 8
Specific gravities are primarily of two types.
Apparent specific gravity
Bulk specific gravity

## Slide 9: Apparent specific gravity
Ratio of the weight of the aggregate (including the impermeable pores) (dried in an oven at 212- 230ºF for 24 hours) to the weight of water occupying a volume equal to that of the solid
Volume of solid includes impermeable pores (but not capillary pores)

## Slide 10: Bulk specific gravity
Bulk specific gravity is defined as the ratio of the weight of a given volume of aggregate, including the permeable and impermeable voids in the particles, to the weight of an equal volume of water.

## Slide 11: Importance of S.G
Specific gravity is a mean to decide the suitability of the aggregate. Low specific gravity generally indicates porous, weak and absorptive materials, whereas high specific gravity indicates materials of good quality.
Specific gravity of major aggregates falls within the range of 2.6 to 2.9.
Specific gravity values are also used while designing concrete mix.

## Slide 12: Bulk Density
It is defined as the weight of the aggregate required to fill a container of unit volume. It is generally expressed in kg/litre.

## Slide 13
Bulk density of aggregates depends upon the following 3 factors.
Degree of compaction
Grading of aggregates
Shape of aggregate particles

## Slide 14: Voids
The empty spaces between the aggregate particles are known as voids.
The volume of void equals the difference between the gross volume of the aggregate mass and the volume occupied by the particles alone.

## Slide 15: Porosity & Absorption
The minute holes formed in rocks during solidification of the molten magma, due to air bubbles, are known as pores. Rocks containing pores are called porous rocks.
Porosity is a ratio of the volume of the pores to the total volume of the particle.
Water absorption may be defined as the difference between the weight of very dry aggregates and the weight of the saturated aggregates with surface dry conditions.

## Slide 16: Fineness Modulus
Fineness modulus is an empirical factor obtained by adding the cumulative percentages of aggregate retained on each of the standard sieves ranging from 80 mm to 150 micron and dividing this sum by 100.
Fineness modulus is generally used to get an idea of how coarse or fine the aggregate is. More fineness modulus value indicates that the aggregate is coarser and small value of fineness modulus indicates that the aggregate is finer.

## Slide 17: Specific Surface of Aggregate
The surface area per unit weight of the material is termed as specific surface.
This is an indirect measure of the aggregate grading.
Specific surface increases with the reduction in the size of aggregate particle.
The specific surface area of the fine aggregate is very much more than that of coarse aggregate.

## Slide 18: Deleterious Materials
Aggregates should not contain any harmful material in such a quantity so as to affect the strength and durability of the concrete. Such harmful materials are called deleterious materials.

## Slide 19
Deleterious materials may cause one of the following effects
To interfere hydration of cement
To prevent development of proper bond
To reduce strength and durability
To modify setting times
Deleterious materials generally found in aggregates, may be grouped as under
Organic impurities
Clay , silt & dust
Salt contamination

## Slide 20: Crushing Value
The aggregates crushing value gives a relative measure of resistance of an aggregate to crushing under gradually applied compressive load.
The aggregate crushing strength value is a useful factor to know the behavior of aggregates when subjected to compressive loads.

## Slide 21: Impact Value
The aggregate impact value gives a relative measure of the resistance of an aggregate to sudden shock or impact.
The impact value of an aggregate is sometime used as an alternative to its crushing value.

## Slide 22: Abrasion Value of Aggregates
The abrasion value gives a relative measure of resistance of an aggregate to wear when it is rotated in a cylinder along with some abrasive charge.

## Slide 23: Mechanical Properties
  Compressive strength
  Toughness
  Abrasion resistance
  Crushing strength

## Slide 24: Toughness
The toughness property test estimates the coarse aggregate resistance to abrasion and mechanical degradation that occurs during handling , construction and service. To perform the test, coarse aggregates larger than 2.36 mm are subjected to impact and grinding by steel spheres. Due to this mechanical degradation, the mass percentage of the coarse material lost gives the toughness. Typically the maximum loss values range from 35 – 45 percent.

## Slide 25: Los Angeles Abrasion Test
A common test used to characterize toughness and abrasion resistance is the Los Angeles (L.A.) abrasion test.
For the L.A. abrasion test, the portion of an aggregate sample is placed in a large rotating drum that contains a shelf plate attached to the outer wall.
A specified number of steel spheres are then placed in the machine and the drum is rotated for 500 revolutions at a speed of 30 - 33 revolutions per minute (RPM).
The material is then extracted and separated into material passing the 1.70 mm (No. 12) sieve and material retained on the 1.70 mm (No. 12) sieve.
The retained material (larger particles) is then weighed and compared to the original sample weight. The difference in weight is reported as a “percent”
Los Angeles Abrasion Machine

## Slide 26: Abrasion Results
Typical results of losses between 10 and 40%.
40% is the max. limit
Coefficient of Variation
  Single Operator – 2%
  Multi lab – 4.5%
Two tests by the same operator on the same sample should not vary by more than 2.83*2.0=5.7% on the % loss (the 2.83 represents 1 in 20 samples outside the range coefficient).
Notes: Using the D2S is common for material testing. Two tests by the same operator on the same sample should not vary by more than 2.83*2.0=5.7% on the % loss (the 2.83 is the one in 20 sample outside the range coefficient). For multiple labs running the same two tests should not vary by more than 2.83*4.5=12.7% on the % loss.

## Slide 27: Other Important Properties
Sr. No. | Aggregate Property | Definition | ASTM Reference
1 | Aggregate Crushing value: | It is the relative measure of the resistance of an aggregate to crushing under a gradually applied compressive load. The method is applicable to aggregate passing a 14.00 mm test sieve and retained on a 10.00mm test sieve. This method is not suitable for testing aggregates with an aggregate crushing value higher than 30 and in such case the method for ten percent fines value. | BS-812-110
2 | Ten Percent fine value | It gives us a relative measure of the resistance of an aggregate to crushing under a gradually applied compressive load. The method is applicable to both weak and strong aggregates passing a 14.00 mm test sieve and retained on 10.00 mm test sieve. | BS-812-111.
3 | Aggregate Impact Value | It’s the relative measure of the resistance of an aggregate to sudden shock or impact. Aggregates ranges from 14.00mm to 10.00 mm size are used | BS-812-112

## Slide 28: Strength of Aggregates
Shale and Sandstone: 35-90 MPa (5-13 ksi)
Limestone: 48-270 MPa (7-39 ksi)
Granite: 27-275 MPa (4-40 ksi)
Pumice: 2 MPa (300 psi)
Traprock: 105-235 MPa (15-34 ksi)