## Slide 1
1
Lecture # 13
Unit: Elastic stress and strain behavior of materials (stress-strain diagram)

## Slide 2: Stress Strain Diagrams
It is a tool for understanding material behavior under load.
A
stress strain diagram
help right
engineers materials
to select the
for specific loading
conditions. Or
It is a graph that represents how a part behaves under an increasing load, and
materials for specific designs.
used by engineers when selecting
2

## Slide 3
A stress-strain diagram generally contains three regions:
Elastic region: This portion is generally represented as a linear relationship between stress and strain. If the load is released the specimen will return to its original dimensions.
Plastic region: In this portion, the specimen begins to yield. The maximum strength of the specimen occurs in this zone. The specimen endures some permanent deformation that remains after the load is released.
Rupture: The point at which a specimen breaks into two parts.

## Slide 5
Stress-strain diagrams are generated experimentally through the performance of controlled tensile tests using fabricated test specimens.
The applied load and displacement are monitored during the test, and are used to calculate stress and strain, respectively.

## Slide 6: Fig: Universal Testing machine

## Slide 8: The stress-strain diagram differs in form for various materials.
•
•
•
•
•
•
Engineering materials are classified as either ductile or brittle materials.
A ductile material is one having relatively large tensile strain up to the point of rupture like structural steel and aluminum.
whereas brittle materials has a relatively small strain up to the point of rupture like cast iron and concrete.
Ductility: Ability of a material to deform under tensile load; high % elongation and % reduction of area indicate ductility.
Brittleness: material failure with little deformation; low % elongation and % reduction of area indicate brittleness.

## Slide 10: Stress-strain Diagram
•
•
•
Proportional Limit (Hooke's Law) : From the origin O to the point P called proportional limit, the stress-strain curve is a straight line.
Force or load is applied axially (no bending)
This linear relation between elongation and the axial force causing was first noticed by Sir Robert Hooke’s in 1678 and is called Hooke's Law.
it states that “within the proportional limit, the stress is directly proportional to strain”.
The constant of proportionality is called the Modulus of Elasticity ‘E’ or Young's Modulus and is equal to the slope of the stress-strain diagram from O to P. Then

## Slide 11
Fig: Stress-strain diagram of a medium- carbon structural steel
12

## Slide 12: Stress-strain Diagram
•
•
•
Modulus of elasticity: To describe elastic properties of linear objects like wires, rods which are stretched or compressed, a convenient parameter is the ratio of the stress to the strain, called the "Young's modulus" or "Modulus of Elasticity" of the material.
Young's modulus can be used to predict the elongation or compression of an object as long as the stress is less than the yield strength of the material.
In many materials, the relation between applied stress and the resulting strain is directly proportional (up to a certain limit),
and a graph representing those two quantities is a straight line. The slope of this line is known as Young’s Modulus, or the
"Modulus of Elasticity."

## Slide 13: The Values of E (Modulus of Elasticity)
S.No Materials | E (GPa)
1. Steel | 200 to 220
2. Cast iron | 100 to 160
3. Copper | 90 to 110
4. Brass | 80 to 90
5. Aluminum | 60 to 80
6. Timber | 10

## Slide 14: Elastic Limit: The limit in which the material will return its original shape when the load is removed.
•
•
•
•
•
Yield Point: Yield point is the point at which the material will have an appreciable elongation OR a slight increase in stress above the elastic limit will result in permanent deformation. This behavior is called yielding for ductile materials (In Engineering, the transition from elastic behavior to plastic behavior).
Less ductile materials such as aluminum and medium to high carbon steels do not have a well defined yield point. For these materials the yield strength is typically determined by “offset method” by which a line is drawn parallel to linear portion of the curve and intersecting at some value most commonly 0.2%. (generally from 0.1% to 0.2%).
Upper yield point: which corresponds to the load reached just before yield starts.
Lower yield point: which corresponding to the load required maintain yield. Lower yield point should be used to determine the yield strength of the material.
.

## Slide 17: Yield strength: you can draw a line parallel to the initial linear portion, and where this line intersects the curve is the yield point. The Y coordinate of this point is the yield strength.
Figure: Yield strength determination

## Slide 18
•
•
•
•
•
Ultimate Strength: The maximum ordinate in the stress-strain diagram is the ultimate strength or tensile strength. This is the maximum load the specimen sustains during the test.
Necking: After the ultimate stress, the cross sectional area begin to decrease in a region of the specimen because of local instability. This phenomenon is known as necking. After necking has been beginning, we note that rupture occurs at an angle of 45 degree with the original surface of the specimen. This indicates that shear stresses are responsible for failure of the ductile materials.
Rapture or Fracture: The specimen spilt into two or more pieces or break into parts.
Rapture Strength: is the strength of the material at rupture. This is also known as the breaking strength.
Strain Hardening: The stress must be increased to keep elongating the specimen, until the maximum value has been reached. This is due to a property of the material known as strain hardening.

## Slide 19
•
•
•
Plasticity or plastic deformation: is the opposite of elastic deformation and is accepted as unrecoverable strain. Plastic deformation is retained even after the relaxation of the applied stress.
Most materials in the linear-elastic category are usually capable of plastic deformation. Brittle materials, like ceramics, do not
experience any plastic deformation and will fracture under relatively low stress.
Consider the difference between a carrot and chewed bubble gum. The carrot will stretch very little before breaking. The chewed bubble gum, on the other hand, will plastically deform enormously before finally breaking.

## Slide 20: Percent Elongation
A standard measure of the ductility of a material is its percent elongation, which is defined as
Percent elongation = ( LB – Lo ) / Lo) 100
Where Lo = Initial length of the tensile test specimen .
LB = Final length at rupture.
For commonly used steels, Standard elongation 21% to 30% are common.

## Slide 21: Percent Reduction
Percent reduction in area = ( Ao –AB ) / Ao) 100
Where Ao = Initial area of the specimen.
AB = Final area at rupture.
For structural steel , percent reduction in area of 60 to 70% are common.
For ductile materials having %E > 5
For brittle materials having % E < 5

## Slide 23: Stress strain diagrams for Brittle m a t e r i als
•
Brittle materials: such as cast iron, glass, concrete and carbon fiber (composite materials) are characterized by the fact that rupture occurs without any prior change in the rate of deformation. These do not have a yield point and do not strain harden, which means that ultimate strength and breaking strength are at same point.

## Slide 24: Stress strain diagrams for Brittle materials
•
From the fig. we note the absence of any necking of the specimen in the case of the brittle materials and observe that rupture occurs along the surface perpendicular to the load. And we conclude that normal stresses are responsible for the failure of brittle materials.

## Slide 25: Stress strain diagrams for Brittle materials Characteristic stress- strain curve for brittle material
0
0.002
0.0048 0.006
375
250
125
0
500
Stress (MPa)
Strain
Gray Cast Iron
Cast Iron

## Slide 26
To calculate the engineering stress, the applied load is divided by the original cross sectional area;
however the true stress would be equal to the load divided by the new deformed cross sectional area.
Therefore true stress > engineering stress.

## Slide 28
Mild steel
Low carbon steel
Medium carbon steel
Aluminum alloys
Cast iron
Glass
copper

## Slide 29
Isotropic materials:
Isotropic materials have elastic properties that are independent of direction. Most common structural materials are isotropic.
Anisotropic materials:
Materials whose properties depend upon direction. An important class of anisotropic materials is fiber-reinforced composites.
Homogeneous
A material is homogeneous if it has the same composition at every point in the body. A homogeneous material may or may not be isotropic.

## Slide 30
Exp: 01:
A hollow cast iron cylinder 4 m long, 300 mm outer diameter and thickness of metal 50 mm is subjected to a central load on the top, when standing straight.
The stress produced is 75 103 KN / m2. Assume E = 1.5 108 KN / m2.
Find (i) magnitude of the load (ii) longitudinal strain produced
(iii) total decrease in length.

## Slide 31: Exp: 1.3:
The following observations were made during a tensile test on mild steel specimen 40 mm in diameter and 200 mm long.
Elongation with 40 KN load (within the limit of proportionality); final diameter = 23. 6 mm
L = 0.0304 mm ; yield load = 161 KN;
Maximum load = 242 KN
Length of specimen at rupture = 249 mm
Determine (a) modulus of elasticity (b) yield point stress (c ) ultimate stress (d) % Elongation (e) % Reduction

## Slide 33: Introduction
33
Mechanical properties that are important to a design engineer differ from those that are of interest to the manufacturing engineer.
In design, mechanical properties such as elastic modulus and yield strength are important in order to resist permanent deformation under applied stresses. Thus, the focus is on the elastic properties.
In manufacturing, the goal is to apply stresses that exceed the yield strength of the material so as to deform it to the required shape. Thus, the focus is on the plastic properties.

## Slide 34: Introduction
34
The yield behavior of a material is determined from the stress-strain relationship under an applied state of stress (tensile, compressive or shear).
This lab introduces the uniaxial tensile test to determine the basic mechanical properties of a material. The main focus of this lab is on the plastic properties of the material.
The test will be conducted in accordance with the standards specified by the American Society for Testing and Materials (ASTM; www.astm.org).

## Slide 35: Terminology
Ductility:
Ductility can be defined as the amount of deformation or strain that the material can withstand before failure. For metal forming processes, increasing the ductility increases the material formability .
In general, the ductility of the specimen is defined in terms of the elongation (EL) or the area reduction (AR) before fracture, i.e.:
35

## Slide 36: Terminology
36
True Stress and Strain:
The true stress () uses the instantaneous or actual area of the specimen at any given point, as opposed to the original area used in the engineering values.
The true strain (ε) is defined as the instantaneous elongation per unit length of the specimen.
The relationship between the true and engineering values is given by:

## Slide 37: Terminology
True Stress and Strain:
Note: For a given value of the load and elongation, the true stress is higher than the Eng. Stress, while the true strain is smaller than the Eng. Strain.
37

## Slide 38: Terminology
38
Strain Hardening:
In the plastic region, the true stress increases continuously. This implies that the metal is becoming stronger as the strain increases. Hence, the name “Strain Hardening”.
The relationship between true stress and true strain
i.e. the flow curve can be expressed using the power law:
where K is called the strength coefficient and n the strain hardening exponent.